Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096516 - RESILIENT SHEET FLOORING

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

SUMMARY

Application:  Refer to BJC Manual of Practice, Flooring Selection Guideline, for application of resilient sheet flooring materials.

This Section specifies resilient sheet flooring for commercial projects.

Vinyl sheet floor covering - backed (SVB)

Vinyl sheet floor covering - unbacked (SVU)

This Section does not specify linoleum floor tile, static-control resilient flooring, resilient sports-floor coverings, or resilient base and accessories.

Edit paragraph below to suit project requirements.  Coordinate with Owner regarding the Preferred Flooring Vendor program.  Refer to Flooring Installation – Scope of Work Checklist for delineation of requirements and responsibilities.

[Contractor, Owner] will engage a flooring contractor for the [demolition,] substrate preparation and installation of flooring materials and systems [, resilient wall base] [resilient moldings] [, wall tiling] [, and resilient stair accessories] through the Owner’s Preferred Flooring Vendor program.  Coordinate responsibilities with Flooring Installation - Scope of Work Checklist.

ACTION SUBMITTALS

Product Data:  For each type of product indicated.

Retain first paragraph below if required.

Shop Drawings:  For each type of floor covering.  Include floor covering layouts, work points, locations of work points, seams, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

Paragraph below assumes manufacturer's standard-size Samples are acceptable.  Revise to suit Project.

Samples:  In manufacturer's standard size, but not less than 6-by-9-inch (150-by-230-mm) sections of each different color and pattern of floor covering required.

INFORMATIONAL SUBMITTALS

Shop Drawings:  For each type of floor covering.  Include floor covering layouts, work points, locations of work points, seams, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

Submit shop drawings to Owner for information.

CLOSEOUT SUBMITTALS

Maintenance data.

QUALITY ASSURANCE

Delete article if fire-test-response testing is not required by authorities having jurisdiction.  In most building codes, resilient floor coverings are exempt from fire-test-response requirements.  See "Fire-Test-Response Characteristics" Article in the Evaluations in Section 096500 "Resilient Flooring" for additional information.

Fire-Test-Response Characteristics:  As determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

Critical Radiant Flux Classification:  Class I, not less than 0.45 W/sq. cm.

PROJECT CONDITIONS

Maintain ambient temperatures within range recommended by manufacturer in spaces to receive floor coverings.

Until Substantial Completion, maintain ambient temperatures within range recommended by manufacturer.

Close spaces to traffic during floor covering installation.

Close spaces to traffic for 48 hours after floor covering installation.

Install floor coverings after other finishing operations, including painting, have been completed.

PRODUCTS

PERFORMANCE REQUIREMENTS

Retain first paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.3; before retaining, verify availability of materials that comply.

FloorScore Compliance:  Resilient sheet flooring shall comply with requirements of FloorScore Standard.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.

VINYL SHEET FLOOR COVERING, BACKED (SVB)

Retain first paragraph below for all renovation and new construction projects.  Retain second paragraph below for projects requiring minor patching and repairing of floor coverings only.

Products[ for new installation and renovation projects]:  Subject to compliance with requirements, available products that may be incorporated into the Work include the following:

Armstrong World Industries, Inc

Mannington Mills, Inc

Tarkett, Inc

Products[ for minor patch or repair projects in limited applications]:  Subject to compliance with requirements, available products that may be incorporated into the Work include the following:

Armstrong World Industries, Inc

Lonseal

Mannington Mills, Inc

Polyflor, Ltd., Distributed by Gerbert Limited

Tarkett, Inc

TOLI International

Vinyl Sheet Floor Covering with Backing:  ASTM F 1303.

Type:  [Type I, minimum binder content of 90 percent] [Type II, minimum binder content of 34 percent].

Wear-Layer Thickness:  Grade 1 only.

Overall Thickness:  [As standard with manufacturer] <Insert thickness>.

Interlayer Material:  [Foamed plastic] [None].

Backing Class:  [Class A (fibrous)] [Class B (nonfoamed plastic)] [Class C (foamed plastic)].

Wearing Surface:  [Smooth] [Embossed] [Smooth with embedded abrasives] [Embossed with embedded abrasives].

Sheet Width:  As standard with manufacturer and as appropriate for intended location to reduce seams.

Colors and Patterns:  Refer to specific facility finish standards.

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Section 096500 "Resilient Flooring" for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

VINYL SHEET FLOOR COVERING, UNBACKED (SVU)

Retain first paragraph below for all renovation and new construction projects.  Retain second paragraph below for projects requiring minor patching and repairing of floor coverings only.

Products[ for new installation and renovation projects]:  Subject to compliance with requirements, available products that may be incorporated into the Work include the following:

Armstrong World Industries, Inc

Mannington Mills, Inc

Tarkett, Inc

Products[ for minor patch or repair projects in limited applications]:  Subject to compliance with requirements, available products that may be incorporated into the Work include the following:

Armstrong World Industries, Inc

Lonseal

Mannington Mills, Inc

Polyflor, Ltd., Distributed by Gerbert Limited

Tarkett, Inc

TOLI International

Unbacked Vinyl Sheet Floor Covering:  ASTM F 1913, [0.080 inch (2.0 mm)] <Insert dimension> thick.

Type:  [Type I, minimum binder content of 90 percent] [Type II, minimum binder content of 34 percent].

Overall Thickness:  [As standard with manufacturer] <Insert thickness>.

Wearing Surface:  [Smooth] [Embossed] [Smooth with embedded abrasives] [Embossed with embedded abrasives].

Sheet Width:  As standard with manufacturer and as appropriate for intended location to reduce seams.

Colors and Patterns:  Refer to specific facility finish standards.

Retain paragraph above or first paragraph below to suit products selected.

INSTALLATION MATERIALS

Trowelable Leveling and Patching Compounds:  Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by manufacturer for applications indicated.

Adhesives:  Water-resistant epoxy-type resin adhesive as recommended by manufacturer to suit floor covering and substrate conditions indicated.

Basis-of-Design Product:  Subject to compliance with requirements, provide Armstrong S-240 High-Performance Epoxy Adhesive (Part A and Part B) or a comparable product:

VOC Content:  Part A and Part B – 10 g/L: calculated and reported, SCAQMD 1168

Integral-Flash-Cove-Base Accessories:

Cove Strip:  1-inch (25-mm) radius provided or approved by manufacturer.

Cap Strip:  Square edge metal cap provided or approved by manufacturer.

Cove height:  Minimum 6” high, coordinate with project specific requirements.

EXECUTION

PREPARATION

Extensive surface preparation is required over substrates from which existing floor coverings have been removed.  Requirements vary among manufacturers.  Insert requirements to suit Project.

Prepare substrates according to manufacturer's written instructions to ensure adhesion of floor coverings.  Coordinate activities with Owner’s infection control requirements.

Manually remove existing flooring and adhesives from existing concrete substrates by scraping method.

Mechanically remove existing flooring and adhesive materials by [grinding,] [and] [sanding] method from existing concrete substrates when materials are not removed by conventional means.

Remove all foreign materials (including but not limited to chemicals, curing compounds, sealers, construction layout markings, etc.) from existing concrete substrates by bead blasting.

Concrete Substrates:  Prepare according to ASTM F 710.

Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by manufacturer.  Do not use solvents.

Alkalinity and Adhesion Testing:  Perform tests recommended by manufacturer.  Proceed with installation only after substrates pass testing.

Moisture Testing:  Perform tests recommended by manufacturer and as follows.  Proceed with installation only after substrates pass all testing.

Follow manufacturer's requirements for moisture testing.  Retain one or both subparagraphs below.

Perform anhydrous calcium chloride test, ASTM F 1869.  Proceed with installation only after substrates have maximum moisture-vapor-emission rate of 3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m) in 24 hours.

Perform relative humidity test using in situ probes, ASTM F 2170.  Proceed with installation only after substrates have a maximum 75 percent relative humidity level measurement.

Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound and remove bumps and ridges to produce a uniform and smooth substrate.

For cracks in substrates that present a vertical offset of greater than 1/8”, notify Owner and Architect prior to patching and repairing.

For depressions in substrates that require floor fill greater than 1/4” thick, refer to Unit Prices.

Do not install floor coverings until they are same temperature as space where they are to be installed.

Mechanical systems shall be in operation at service temperature for 72 hours prior to installation and for duration of the project.

Move floor coverings and installation materials into spaces where they will be installed at least 48 hours in advance of installation.

Floor coverings shall be unpackaged and stored in a relaxed state prior to installation in accordance with manufacturer’s requirements.

Sweep and vacuum clean substrates to be covered by floor coverings immediately before installation.

FLOOR COVERING INSTALLATION

Comply with manufacturer's written instructions for installing floor coverings.

Unroll floor coverings and allow them to stabilize before cutting and fitting.

Lay out floor coverings as follows:

Maintain uniformity of floor covering direction.

Minimize number of seams; place seams in inconspicuous and low-traffic areas, at least 6 inches (152 mm) away from parallel joints in floor covering substrates.

Match edges of floor coverings for color shading at seams.

Avoid cross seams.

If required, insert requirements for special patterns here.

If built-in items are required to be set on top of floor coverings, indicate on Drawings and revise first paragraph below.

Scribe and cut floor coverings to butt neatly and tightly to vertical surfaces, permanent fixtures, and built-in furniture including cabinets, pipes, outlets, and door frames.

Extend floor coverings into toe spaces, door reveals, closets, and similar openings.

Maintain reference markers, holes, or openings that are in place or marked for future cutting by repeating on floor coverings as marked on substrates.  Use chalk or other nonpermanent marking device.

Adhere floor coverings to substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

Integral-Flash-Cove Base:  Cove floor coverings 6 inches (152 mm) unless otherwise dimension indicated up vertical surfaces.  Support floor coverings at horizontal and vertical junction by cove strip.  Butt at top against cap strip.

CLEANING AND PROTECTION

Comply with manufacturer's written instructions for cleaning and protection of floor covering.

Before retaining first paragraph below, verify manufacturer's floor polish recommendations.  Floor polish is used with most vinyl sheet floor coverings.

Floor Polish:  Provided by owner in accordance with manufacturers recommendations.

Cover floor coverings until Substantial Completion.

END OF SECTION 096516