Copyright 2013 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 099123 - INTERIOR PAINTING

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

SUMMARY

Section includes surface preparation and the application of paint systems on interior substrates.

Retain paragraph below to clarify scope of work requirements if necessary.

Scope of Work.

Finish interior surfaces exposed to view and without a factory finish, unless otherwise indicated.

Finish both faces and all edges of plywood backboards in electrical, mechanical, and telecommunication rooms.

Prime surfaces to receive wall coverings.

Mechanical and electrical equipment exposed to view in areas

DEFINITIONS

Retain this article if paints are specified by manufacturers' trade names rather than by MPI paint numbers. Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

Retain terms that remain after this Section has been edited for a project.

MPI Gloss Level 1: Not more than five units at 60 degrees and 10 units at 85 degrees, according to ASTM D 523.

MPI Gloss Level 2: Not more than 10 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D 523.

MPI Gloss Level 3: 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D 523.

MPI Gloss Level 4: 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, according to ASTM D 523.

MPI Gloss Level 5: 35 to 70 units at 60 degrees, according to ASTM D 523.

MPI Gloss Level 6: 70 to 85 units at 60 degrees, according to ASTM D 523.

MPI Gloss Level 7: More than 85 units at 60 degrees, according to ASTM D 523.

ACTION SUBMITTALS

Product Data: For each type of product. Include preparation requirements and application instructions.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

Include Printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

Samples: For each type of paint system and in each color and gloss of topcoat.

QUALITY ASSURANCE

Mockups: Apply mockups of each paint system indicated and each color and finish selected to verify preliminary selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

Architect will select one surface to represent surfaces and conditions for application of each paint system.

Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

Other Items: Architect will designate items or areas required.

Final approval of color selections will be based on mockups.

If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or ARCOM. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

MANUFACTURERS

Retain "Products" Paragraph below and insert lists of manufacturers and products in Interior Painting Schedule to require specific products or a comparable product from other manufacturers.

See lists of products currently approved by MPI in its "MPI Approved Products Lists." See "Writing Guide" Article in the Evaluations for further discussion.

Products: Subject to compliance with requirements, provide products manufactured by the Sherwin-Williams Company.

PAINT, GENERAL

MPI Standards: Products shall comply with MPI standards indicated and shall be listed in its "MPI Approved Products Lists."

Material Compatibility:

Systems could fail if paints used for individual coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

Materials for use within each paint system shall be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

For each coat in a paint system, products shall be recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

Retain second option in "VOC Content" Paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit EQ 4.2; coordinate with products. For names of products that comply, see products listed as complying with LEED VOC limits on "MPI Approved Products Lists."

VOC Content: Products shall comply with VOC limits of authorities having jurisdiction and, for interior paints and coatings applied at Project site, the following VOC limits, exclusive of colorants added to a tint base:

Flat Paints and Coatings: 50 g/L.

Nonflat Paints and Coatings: 150 g/L.

Dry-Fog Coatings: 400 g/L.

Primers, Sealers, and Undercoaters: 200 g/L.

Anticorrosive and Antirust Paints Applied to Ferrous Metals: 250 g/L.

Zinc-Rich Industrial Maintenance Primers: 340 g/L.

Pretreatment Wash Primers: 420 g/L.

Floor Coatings: 100 g/L.

Shellacs, Clear: 730 g/L.

Shellacs, Pigmented: 550 g/L.

Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

[Ten] [Twenty] [Thirty] <Insert number> percent of surface area will be painted with deep tones.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in six subparagraphs below are based on "MPI Manual."

Concrete: 12 percent.

Fiber-Cement Board: 12 percent.

Masonry (Clay and CMUs): 12 percent.

Wood: 15 percent.

Gypsum Board: 12 percent.

Plaster: 12 percent.

Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers.

Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of surfaces and conditions.

PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Interior Painting Schedule.

Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

APPLICATION

Apply paints according to manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual."

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

INTERIOR PAINTING SCHEDULE

Paint systems in this article are based on "MPI Architectural Painting Specification Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

CMU Substrates:

Latex System [MPI INT 4.2A]:

Block Filler: Block filler, latex, interior/exterior[, MPI #4].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Latex Aggregate System [MPI INT 4.2B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: Primer for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Intermediate Coat: Intermediate coat for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Retain one of two "Topcoat" subparagraphs below.

Topcoat: Textured coating, latex, nonflat[, MPI #41].

<Insert manufacturer's name; product name or designation>.

Topcoat: Textured coating, latex, flat[, MPI #42].

<Insert manufacturer's name; product name or designation>.

Institutional Low-Odor/VOC Latex System [MPI INT 4.2E]:

Block Filler: Block filler, latex, interior/exterior[, MPI #4].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level 5)[, MPI #147].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

<Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System [MPI INT 4.2D] [MPI INT 4.2P]:

Retain "Block Filler" or "Prime Coat" Subparagraph below. First corresponds to MPI INT 4.2D; second corresponds to MPI INT 4.2P.

Block Filler: Block filler, latex, interior/exterior[, MPI #4].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkali resistant, water based[, MPI #3].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level 5)[, MPI #141].

<Insert manufacturer's name; product name or designation>.

Water-Based Light Industrial Coating System [MPI INT 4.2K]:

Block Filler: Block filler, latex, interior/exterior[, MPI #4].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Light industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, semi-gloss (MPI Gloss Level 5)[, MPI #153].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

<Insert manufacturer's name; product name or designation>.

For areas subject to wetting, consider using epoxy system MPI INT 4.2G, which is specified in Section 099600 "High-Performance Coatings," instead of alkyd system in "Alkyd System" Subparagraph below.

Alkyd System [MPI INT 4.2C] [MPI INT 4.2N]:

Block Filler: Block filler, latex, interior/exterior[, MPI #4].

<Insert manufacturer's name; product name or designation>.

Retain "Sealer Coat" Subparagraph below for MPI INT 4.2N; delete for MPI INT 4.2C.

Sealer Coat: Primer sealer, latex, interior[, MPI #50].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level 5)[, MPI #47].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

<Insert manufacturer's name; product name or designation>.

Steel Substrates:

Latex System, Alkyd Primer [MPI INT 5.1Q] [MPI INT 5.1QQ]:

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1Q; second corresponds to MPI INT 5.1QQ. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Latex over Shop-Applied Quick-Drying Shop Primer System [MPI INT 5.1X]:

Prime Coat: Primer, quick dry, for shop application[, MPI #275].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Institutional Low-Odor/VOC Latex System [MPI INT 5.1S]:

Prime Coat: Primer, rust inhibitive, water based[ MPI #107].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level 5)[, MPI #147].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

<Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System [MPI INT 5.1R] [MPI INT 5.1R]:

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1R; second corresponds to MPI INT 5.1RR. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level 5)[, MPI #141].

<Insert manufacturer's name; product name or designation>.

Water-Based Light Industrial Coating System [MPI INT 5.1B]:

Prime Coat: Primer, rust-inhibitive, water based[ MPI #107].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Light industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, semi-gloss (MPI Gloss Level 5)[, MPI #153].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

<Insert manufacturer's name; product name or designation>.

Water-Based Dry-Fall System [MPI INT 5.1C] [MPI INT 5.1CC]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1C; second corresponds to MPI INT 5.1CC. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Dry fall, latex, flat[, MPI #118].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level 1)[, MPI #133].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, latex (MPI Gloss Level 3)[, MPI #155].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, latex (MPI Gloss Level 5)[, MPI #226].

<Insert manufacturer's name; product name or designation>.

Alkyd System [MPI INT 5.1E] [MPI INT 5.1EE]:

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1E; second corresponds to MPI INT 5.1EE. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level 5)[, MPI #47].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

<Insert manufacturer's name; product name or designation>.

Alkyd over Surface-Tolerant Primer System [MPI INT 5.1T]:

Prime Coat: Primer, metal, surface tolerant[ MPI #23].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level 5)[, MPI #47].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

Quick-Dry Enamel System [MPI INT 5.1A]:

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

Topcoat: Alkyd, quick dry, semi-gloss (MPI Gloss Level 5)[, MPI #81].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, quick dry, gloss (MPI Gloss Level 7)[, MPI #96].

<Insert manufacturer's name; product name or designation>.

Alkyd Dry-Fall System [MPI INT 5.1D] [MPI INT 5.1DD]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1D; second corresponds to MPI INT 5.1DD. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Dry fall, alkyd, flat[, MPI #55].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, alkyd (MPI Gloss Level 3)[, MPI #89].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, alkyd, semi-gloss (MPI Gloss Level 5)[, MPI #225].

<Insert manufacturer's name; product name or designation>.

Aluminum Paint System [MPI INT 5.1M] [MPI INT 5.1MM]:

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.1M; second corresponds to MPI INT 5.1MM. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint[, MPI #1].

<Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

Galvanized-Metal Substrates:

Latex System [MPI INT 5.3A]:

Prime Coat: Primer, galvanized, water based[, MPI #134].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Institutional Low-Odor/VOC Latex System [MPI INT 5.3N]:

Prime Coat: Primer, galvanized, water based[, MPI #134].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level 5)[, MPI #147].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

<Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System [MPI INT 5.3M]:

Prime Coat: Primer, galvanized, water based[, MPI #134].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level 5)[, MPI #141].

<Insert manufacturer's name; product name or designation>.

Water-Based Light Industrial Coating System MPI INT 5.3B:

Prime Coat: Primer, galvanized, water based[, MPI #134].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Light industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, semi-gloss (MPI Gloss Level 5)[, MPI #153].

<Insert manufacturer's name; product name or designation>.

Topcoat: Light industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

<Insert manufacturer's name; product name or designation>.

Water-Based Dry-Fall System [MPI INT 5.3H]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Prime Coat: Dry fall, water based, for galvanized steel, matching topcoat.

Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level 1)[, MPI #133].

<Insert manufacturer's name; product name or designation>.

Alkyd over Cementitious Primer System [MPI INT 5.3C]:

Prime Coat: Primer, galvanized, cementitious[, MPI #26].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level 5)[, MPI #47].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

<Insert manufacturer's name; product name or designation>.

Alkyd Dry-Fall System (Cementitious Primer) [MPI INT 5.3F]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Prime Coat: Primer, galvanized, cementitious[, MPI #26].

<Insert manufacturer's name; product name or designation>.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Dry fall, alkyd, flat[, MPI #55].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, alkyd (MPI Gloss Level 3) [, MPI #89].

<Insert manufacturer's name; product name or designation>.

Topcoat: Dry fall, alkyd, semi-gloss (MPI Gloss Level 5)[, MPI #225].

<Insert manufacturer's name; product name or designation>.

Aluminum Paint System (Cementitious Primer) [MPI INT 5.3G]:

Prime Coat: Primer, galvanized, cementitious[, MPI #26].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint[, MPI #1].

<Insert manufacturer's name; product name or designation>.

[Gypsum Board] [and] [Plaster] Substrates:

Latex over Latex Sealer System [MPI INT 9.2A]:

Retain one of two "Prime Coat" subparagraphs below. Retain first for a Premium Grade system.

Prime Coat: Primer sealer, latex, interior[, MPI #50].

<Insert manufacturer's name; product name or designation>.

Prime Coat: Latex, interior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Latex over Alkyd Primer System (for Plaster Only) [MPI INT 9.2K]:

Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5)[, MPI #54].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

<Insert manufacturer's name; product name or designation>.

Institutional Low-Odor/VOC Latex System [MPI INT 9.2M]:

Prime Coat: Primer sealer, interior, institutional low odor/VOC[, MPI #149].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level 5)[, MPI #147].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

<Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System [MPI INT 9.2B]:

Prime Coat: Primer sealer, latex, interior[, MPI #50].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

<Insert manufacturer's name; product name or designation>.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level 5)[, MPI #141].

<Insert manufacturer's name; product name or designation>.

Alkyd over Latex Sealer System [MPI INT 9.2C]:

Prime Coat: Primer sealer, latex, interior[, MPI #50].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level 5)[, MPI #47].

<Insert manufacturer's name; product name or designation>.

Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

<Insert manufacturer's name; product name or designation>.

END OF SECTION 099123